## Slide 1: Key findings
We revealed unexpected formation of 1D metal-organic chains (MOC) comprised of circumcoronene monomers coordinated by single Cu adatoms on Cu(111) surface.
MOC formation implies unusual highly-efficient and regioselective activation C-H bonds located at zigzag edges.
With aid of CO-functionalized imaging we confirm presence of single Cu coordination atom and bent geometry of the circumcoronene monomers.
dI/dV imaging with CO-tip enabled resolution of frontier orbitals (HOMO, LUMO and [LUMO+1]) and their hybridization with Cu adatom states (HOMO+Cu and [LUMO+1]+Cu).
We observe reversible transformation of MOC to individual circumcoronene molecules upon annealing in atomic H flux.
Stability and formation of MOC is driven by cooperative effect of i) lowered barrier for C-H bond dissociation facilitated by presence of Cu adatom ; ii) unique molecule’s symmetry and aromaticity (7 Clar’s sextets) reinforcing its ability to accommodate strained bent geometry within MOC registered with Cu(111) substrate.
Notes: Q (JH): Previous image shows coordinated by 3 Cu atoms? See the other PPT on slides 1 and 3.

## Slide 2
Cu
270C
1 hour
Cu
Cu
T>>270C
Or prolonged annealing
Cu
Cu
M. Telychko, G. Li et al Science Advances 7(3), eabf0269, 2021
Notes: Dimerization vs. polymerization?

## Slide 3
Formation of circumcoronene-based Cu-coordinated metal-organic (MOC) chains
60x60nm, 1V, 500pA
MO dimer
90x90nm, 1V, 1nA
1200
60x60nm, 1V, 500pA
275C
2 hours
310C
2 hours
1V, 1nA 60x50nm
270C
Overnight anneal
(14 hours)
Notes: There is good C6-Cu registry.

## Slide 4
13x13nm, .9V, 1.5nA
13x13nm, 1V, 1nA
CO tip
CO
CO absorbed
Metallic tip
CO
MO dimer
Circumcoronene
c
o
Notes: Dimer shows an offset; really dimerized with Cu in between? No offset with a little rotation.

## Slide 5
dI/dV@0.7V
0.9V
1.15V
1.25V
1.35V
1.45V
1.50V
1.60V
1.70V
1.80V
1.90V
-1.60V
-1.30V
-1.40V
dI/dV mapping with CO-tip: HOMO, HOMO+Cu, LUMO, [LUMO+1]+Cu, LUMO+1

## Slide 6
Cu(111)
Trimer
Circumcoronene
Dimer
Circ.
Dimer
Trimer
HOMO
LUMO
LUMO+1
dI/dV  HOMO, LUMO and LUMO+1 “circumcoronene” orbitals
HOMO (V) | LUMO
-1.7 | 0.82
-1.65 | 0.73
-1.6 | 0.68
-1.6 | 0.68
Teramer
dI/dV @LUMO
dI/dV @ LUMO+1
dI/dV @HOMO
Topo.

## Slide 7
Cu(111)
Trimer
Circumcoronene
Dimer
dI/dV
(LUMO+1) + Cu
1.25V
dI/DV
@ HOMO+ Cu
[LUMO+1]+Cu
HOMO+ Cu
dI/dV  additional states derived from HOMO/(LUMO+1) orbitals and Cu adatom d orbitals.

## Slide 8
Constant. Current ncAFM
Cu
Cu
Laplace filtered Current channel
Laplace filtered Current channel
Bond resolved imaging -> molecules adopt bent concave-like geometry
Constant-current STM
50mV, 0.4nA

## Slide 9
100mV, 0.5nA
70mV, 0.5nA
Const. Current ncAFM
Constant-current STM
Constant-current ncAFM
Bond resolved imaging -> molecules adopt bent concave-like geometry

## Slide 10
Constant current STM Constant currentncAFM
Constant height ncAFM
Bond resolved imaging -> molecules adopt bent concave-like geometry

## Slide 11: Annealing with atomic H flux -> reversible transformation of MO chains to individual circumcoronenes
1V, 1nA 60x50nm
20nm
Before
After (same sample annealed @ 270C + atomic H)
1V, 1nA 30x30nm
270C +
atomic H
270C +
atomic H
Notes: What calculations should we perform to differentiate from the Mykola’s previous Angew Chem and Sci Adv papers?